**Tender Stilmat Code™ Standard**

|  |  |
| --- | --- |
| Description Model | Special and high quality Dust Control Carpet mat, rug or inlay, for covered and indoor areas.  Suitable for intensive covered and indoor foot traffic, where moisture absorption and dirt scraping are key considerations. CODE STILMAT - doormat, rug, inlay |
| Code | CO-DCC |
| Characteristics | Indoor, super absorbing and scraping |
| Pile material | 100% Polyamide |
| Backing | PVC |
| Primary backing | Nonwowen PET/PA |
| Yarn construction | Velour |
| Pattern | Blended |
| Total weight ISO 8543 | Min 3.600 gram/m² |
| Total height ISO 1765 | Min. 8.5 mm |
| Use classification EN 1307 | Min. 33 |
| Wearing class EN 1963 | Min. 33 |
| Comfort EN 1307 | Min. LC2 |
| Traffic class | Recommended for high intensive foot traffic |
| Absorption capacity TNO W6034 | Min. 5.0 l/m² |
| Flammability Euroclass EN13501 | Min. Cfl /s1 |
| Slip Resistance EN13893 | Min. DS |
| Sand absorption 1-3 | Min. 3 |
| Optical class 1-5 | Min. 4.5 |
| Sizes rolls | Up to 2000mm Width, 25000mm length  |
| Rubber border/edge | Upon request |
| Quality class | 33 For Luxury and commercial buildings |
| Ideal position on entrance | Covered or indoor space with high traffic |
| Zone: I – II – III | II, III  |
| Country of origin  | Netherlands (EU) |
| Contact | STILMAT |