Tender Lombok standard

|  |  |
| --- | --- |
| Description | Special and high quality ribbed carpet mat inlay, for covered and indoor areas.  Suitable for intensive covered and indoor foot traffic, where moisture absorption and dirt scraping are key considerations. |
| Model | LOOMBOK® - Ribbed carpet inlay for STILMAT® doormats |
| Code | LB |
| Characteristics | Indoor ribbed premium carpet with gel |
| Standard VOC | A+ |
| Pile material | 100% Polypropiene |
| Backing | Latex gel |
| Primary backing | Nonwowen PP |
| Yarn construction | Ribbed/Cut-loop |
| Pattern | Blended |
| Total weight ISO 8543 | Min 2.100 gram/m² |
| Total height ISO 1765 | Min. 10 mm |
| Traffic class | Recommended for high intensive foot traffic |
| Absorption capacity  | High |
| Flammability  | EFL |
| Slip Resistance EN13893 | DS |
| Sizes rolls | Up to 2000mm Width, 25000mm length  |
| Rubber border/edge | Upon request |
| Quality class | For Luxury and commercial buildings |
| Ideal position on entrance | Covered or indoor space with high traffic |
| Zone: I – II – III | II, III  |
| Country of origin | Belgium (EU) |
| Contact | STILMAT |