Tender Stilmat™ Master brush

|  |  |
| --- | --- |
| Description | Master brush STILMAT is special outdoor mat, that pairs scraping qualities with moisture absorption. Textile look. It has characteristics of STILMAT lux brushes and it changes any rubber, brush or carpet mat or inlay. Weather resistant. |
| Model | MATER BRUSH STILMAT - doormat, rug, inlay |
| Code | MB-DCC |
| Characteristics  | Outdoor, super absorbing and scraping |
| Pile material | 100% Polyamide |
| Backing | PVC |
| Primary backing | Nonwowen PET/PA |
| Yarn construction | Bouclé construction |
| Pattern | Blended |
| Total weight ISO 8543 | Min 2.950 gram/m² |
| Total height ISO 1765 | Min. 8.5 mm |
| Use classification EN 1307 | Min. 33 |
| Wearing class EN 1963 | Min. 33 |
| Comfort EN 1307 | Min. LC1 |
| Traffic class | Recommended for high intensive foot traffic |
| Absorption capacity TNO W6034 | Min. 3.7 l/m² |
| Flammability Euroclass EN13501 | Min. Cfl /s1 |
| Slip Resistance EN13893 | Min. DS |
| Sand absorption 1-3 | Min. 2 |
| Optical class 1-5 | Min. 4.5 |
| Sizes rolls | Up to 2000mm Width, 25000mm length  |
| Rubber border/edge | Upon request |
| Quality class | For Luxury and commercial buildings |
| Ideal position on entrance | Outdoor or covered space with high traffic |
| Zone: I – II – III | I, II  |
| Country of origin | Netherlands (EU) |
| Contact | STILMAT |