Tender Performance FG

|  |  |
| --- | --- |
| Description | Highest level of non flammability in our offer (Bfl-s1). Premium quality. Excellent performance of absorbing and scraping for entrance matting, rug or inlay. It provides excellent wear resistance and is extremely suitable for heavy duty commercial applications. |
| Model | PERFORMANCE STILMAT – Fire guard - doormat, rug, inlay |
| Code | PF-DCCFG |
| Characteristics | Indoor, super absorbing and scraping |
| Pile material | 100% recycled (Econyl®) Polyamide |
| Backing | PVC |
| Primary backing | Nonwowen PET/PA |
| Yarn construction | Velour |
| Pattern | Mixed |
| Total weight ISO 8543 | Min 3.650 gram/m² |
| Total height ISO 1765 | Min. 7.5 mm |
| Use classification EN 1307 | Min. 33 |
| Wearing class EN 1963 | Min. 33 |
| Comfort EN 1307 | Min. LC3 |
| Traffic class | Recommended for high intensive foot traffic |
| Absorption capacity TNO W6034 | Min. 4.7 l/m² |
| Flammability Euroclass EN13501 | Min. Bfl /s1 |
| Slip Resistance EN13893 | Min. DS |
| Sand absorption 1-3 | Min. 3 |
| Optical class 1-5 | Min. 4.5 |
| Sizes rolls | Up to 2000 mm width, 25000 mm length  |
| Rubber border/edge | Upon request |
| Quality class | For Luxury and commercial buildings |
| Ideal position on entrance | Covered or indoor space with high traffic |
| Zone: I – II – III | II, III  |
| Country of origin | Netherlands (EU) |
| Contact | STILMAT |