Tender Performance GC

|  |  |
| --- | --- |
| Description | Eco-Friendly carpet which is in accordance with A+,VOC, EMS and LEED standard. Premium quality. Excellent performance of absorbing and scraping for entrance matting, rug or inlay. It provides excellent wear resistance and is extremely suitable for heavy duty commercial applications. |
| Model | PERFORMANCE STILMAT – Green concept - doormat, rug, inlay |
| Code | PF-DCCGC |
| Characteristics | Indoor, super absorbing and scraping |
| Pile material | 100% recycled (Econyl®) Polyamide |
| Backing | PU (PVC FREE) |
| Primary backing | Nonwowen PET/PA |
| Yarn construction | Velour |
| Pattern | Mixed |
| Total weight ISO 8543 | Min 2.750 gram/m² |
| Total height ISO 1765 | Min. 7.5 mm |
| Use classification EN 1307 | Min. 33 |
| Wearing class EN 1963 | Min. 33 |
| Comfort EN 1307 | Min. LC3 |
| Traffic class | Recommended for high intensive foot traffic |
| Absorption capacity TNO W6034 | Min. 4.7 l/m² |
| Flammability Euroclass EN13501 | Min. Cfl /s1 |
| Slip Resistance EN13893 | Min. DS |
| Sand absorption 1-3 | Min. 3 |
| Optical class 1-5 | Min. 4.5 |
| Sizes rolls | Up to 2000 mm width, 25000 mm length |
| Rubber border/edge | Upon request |
| Quality class | For Luxury and commercial buildings |
| Ideal position on entrance | Covered or indoor space with high traffic |
| Zone: I – II – III | II, III |
| Country of origin | Netherlands (EU) |
| Contact | STILMAT |