Tender Premium Standard

|  |  |
| --- | --- |
| Description | The mat features a bouclé construction. In this kind of composition the pile material is formed out of looped pile. Combined with the blended design this makes small patches of dirt invisible. The strong and resistant pile is made up of different yarns to allow moisture absorption and dirt scraping. |
| Model | PREMIUM STILMAT - doormat, rug, inlay |
| Code | PR-DCC |
| Characteristics | Indoor, super absorbing and scraping |
| Pile material | 100% Polyamide |
| Backing | PVC |
| Primary backing | Nonwoven PET/PA |
| Yarn construction | Bouclé |
| Pattern | Blended |
| Total weight ISO 8543 | Min 3.550 gram/m² |
| Total height ISO 1765 | Min. 7.0 mm |
| Use classification EN 1307 | Min. 32 |
| Wearing class EN 1963 | Min. 32 |
| Comfort EN 1307 | Min. LC3 |
| Traffic class | Recommended for high intensive foot traffic |
| Absorption capacity TNO W6034 | Min. 5.1 l/m² |
| Flammability Euroclass EN13501 | Min. Cfl /s1 |
| Slip Resistance EN13893 | Min. DS |
| Sand absorption 1-3 | Min. 2 |
| Optical class 1-5 | Min. 4.5 |
| Sizes rolls | Up to 2000mm Width, 25000mm length |
| Rubber border/edge | Upon request |
| Quality class | For Luxury and commercial buildings |
| Ideal position on entrance | Covered or indoor space with high traffic |
| Zone: I – II – III | II, III |
| Country of origin | Netherlands (EU) |
| Contact | STILMAT |