Tender Prestige Standard

|  |  |
| --- | --- |
| Description | Special and high quality Dust Control Carpet rug for covered and indoor areas. The PRESTIGE STILMAT™ is indoor durable mat, runner or inlay, with luxurious character. The mat is ideal for high moisture absorption. |
| Model | PRESTIGE STILMAT - doormat, rug, inlay |
| Code | PS-DCC |
| Characteristics  | Indoor, super absorbing and scraping  |
| Pile material | 100% Polyamide |
| Backing | PVC |
| Primary backing | Nonwoven PET/PA |
| Yarn construction |  Velour |
| Pattern | Blended |
| Total weight ISO 8543 | Min 3.650 gram/m² |
| Total height ISO 1765 | Min. 8.5 mm |
| Use classification EN 1307 | Min. 32 |
| Wearing class EN 1963 | Min. 33 |
| Comfort EN 1307 | Min. LC3 |
| Traffic class | Recommended for high intensive foot traffic |
| Absorption capacity TNO W6034 | Min. 6.3 l/m² |
| Flammability Euroclass EN13501 | Min. Cfl /s1 |
| Slip Resistance EN13893 | Min. DS |
| Sand absorption 1-3 | Min. 2 |
| Optical class 1-5 | Min. 4 |
| Sizes rolls | Up to 2000 mm Width, 25000 mm length |
| Rubber border/edge | Upon request |
| Quality class | For Luxury and commercial buildings |
| Ideal position on entrance | Covered or indoor space with high traffic |
| Zone: I – II – III | II, III  |
| Country of origin | Netherlands (EU) |
| Contact | STILMAT |